# Background: Halide Perovskite Semiconductors for Radiation Detection

The research reported in Chapters [ch:CsFAPbI] and [ch:perovskite_detectors] rests on three intersecting bodies of knowledge: the crystal chemistry and electronic structure of halide perovskites, the physics governing how ionizing radiation deposits energy in matter, and the device physics that determines how efficiently that deposited energy is converted into a measurable electrical signal. This chapter develops each body of knowledge in sufficient depth to motivate the experimental choices made in later chapters and to place the results in the context of the broader literature on semiconductor radiation detectors. The FPGA-based systems work is treated separately in Chapter [ch:FPGA_background].

## The Perovskite Crystal Structure and Material Families

### The ABX​3 Archetype

The term “perovskite” derives from the mineral calcium titanate (CaTiO​3), named for the Russian mineralogist Lev von Perovski and first synthesized in the nineteenth century . The defining structural motif is a three-dimensional network of corner-sharing BX​6 octahedra in which a larger A-site cation occupies the 12-coordinate cuboctahedral void at the unit-cell body-center (in the ideal cubic setting, space group Pm3m). The versatility of this archetype arises from the wide range of chemistries that can be accommodated without destroying the framework: in the oxide family, B-sites range from Ti​4+ to Pb​4+, while in the halide family addressed here, B is almost exclusively Pb​2+ (or Sn​2+) and X is a monovalent halide (I​−, Br​−, or Cl​−).

The stability of a given ABX​3 composition is conveniently predicted by the Goldschmidt tolerance factor,

$$\begin{equation}
      t = \frac{r_{\rm A} + r_{\rm X}}{\sqrt{2}\,(r_{\rm B} + r_{\rm X})},
      \label{eq:tolerance}
    \end{equation}$$

where ri denotes the ionic radius of species i . Perovskite formation is generally favored for 0.80≤t≤1.05; values close to unity favor the ideal cubic structure, while smaller values drive cooperative octahedral tilting that lowers the symmetry to tetragonal or orthorhombic phases. Kieslich et al. extended this framework to hybrid organic-inorganic systems by defining effective radii for polyatomic organic cations from the root-mean-square displacement of their hydrogen envelope , enabling quantitative phase stability predictions for the methylammonium and formamidinium compounds central to this work.

A complementary criterion is the octahedral factor $\mu = r_{\rm B}/r_{\rm X}$, which must satisfy 0.414≤μ≤0.732 for the B cation to fit stably inside the halide octahedron. Pb​2+ (r=1.19 Å) paired with I​− (r=2.20 Å) gives μ=0.54, comfortably within the stable range and consistent with the broad tunability of the Pb-halide framework.

### Three-Dimensional Structures

Methylammonium lead iodide (MAPbI​3). The most extensively studied hybrid halide perovskite, MAPbI​3 (methylammonium = CH​3NH​3+, MA​+), adopts a cubic structure above 327 K, a tetragonal structure between 162 K and 327 K, and an orthorhombic structure below 162 K . At room temperature, the tetragonal phase (space group I4/mcm) is therefore the operative structure for detector applications. MAPbI​3 has a direct bandgap of approximately 1.55 eV and a high optical absorption coefficient (>104 cm​−1 above the bandgap), along with the excellent charge transport described in Section 1.4.2. Large single crystals with centimeter-scale dimensions can be grown from solution by inverse temperature crystallization , making bulk detector fabrication feasible. The principal weakness of MAPbI​3 for detector applications is the light A-site cation: the low atomic masses of C, N, and H contribute minimally to gamma-ray stopping power, and the modest hydrogen density in the cubic CH​3NH​3+ cation limits fast-neutron response. The MAPbI​3-hBN composite detector described in Chapter [ch:perovskite_detectors] addresses the neutron sensitivity limitation by incorporating high-n boron-containing nanoflakes within a MAPbI​3 matrix.

Cesium lead bromide (CsPbBr​3). Replacing the organic MA​+ cation with the monoatomic Cs​+ (r=1.67 Å) yields an all-inorganic perovskite with significantly improved thermal and photochemical stability . CsPbBr​3 undergoes orthorhombic-to-tetragonal (∼88 ​∘C) and tetragonal-to-cubic (∼130 ​∘C) transitions, remaining in the orthorhombic phase at room temperature. Its bandgap of approximately 2.3 eV is wide enough to suppress intrinsic carrier excitation at 300 K, yielding resistivities exceeding 109 Ω cm in single crystals , a prerequisite for the low dark-current operation required in radiation counting. Most critically for gamma detection, the presence of both Cs (Z=55) and Pb (Z=82) gives CsPbBr​3 a calculated effective atomic number of approximately 65.9, far exceeding that of conventional detector materials such as silicon ($Z_{\rm eff} = 14$) and approaching that of cadmium zinc telluride ($Z_{\rm eff} \approx 49.1$) . This high $Z_{\rm eff}$ makes CsPbBr​3 among the most promising semiconductor candidates for room-temperature gamma spectroscopy.

Mixed cation Cs​0.1FA​0.9PbI​3. Pure formamidinium lead iodide (FAPbI​3, FA​+ = CH(NH​2)​2+) has a narrower bandgap of approximately 1.48 eV and superior thermal stability relative to MAPbI​3, but the desired black α-phase is metastable at room temperature, spontaneously converting to the photoinactive yellow δ-phase . Partial substitution of FA​+ with Cs​+ (typically 5–15 mol%) suppresses this phase transition by reducing the tolerance factor toward unity, entropy-stabilizing the cubic α-phase at ambient conditions . The composition Cs​0.1FA​0.9PbI​3 investigated in Chapter [ch:CsFAPbI] exploits this stabilization while retaining the narrow bandgap and large absorption cross-section of FAPbI​3, enabling its use as a photon-responsive active layer in a photovoltaic architecture repurposed as a radiation monitor.

### Two-Dimensional Ruddlesden-Popper Structures

The three-dimensional perovskite framework can be sliced along specific crystallographic planes and the resulting slabs separated by layers of large organic spacer cations to form two-dimensional (2D) or quasi-2D structures. In the Ruddlesden-Popper series the general formula is (R)2(MA)​n−1Pb​nX​3n+1, where R is a large organic cation that cannot fit the A-site of the 3D structure, n is the number of corner-sharing PbX​6 octahedral layers between adjacent organic spacer bilayers, and the ratio of inorganic to organic content increases with n . In the limit n→∞ the three-dimensional structure is recovered.

For the present work, the relevant composition is the n=3 member PEA​2MA​2Pb​3I​10, where PEA​+ denotes the phenylethylammonium cation (C​6H​5(CH​2)​2NH​3+). The alternating organic-inorganic layering creates a natural quantum-well electrostatic landscape in which charge is preferentially confined within the higher-dielectric inorganic slabs. From a detector perspective, this layered architecture confers two important advantages over its 3D counterpart: the bulky PEA​+ layers act as physical barriers to halide vacancy migration, substantially suppressing the ion-transport instabilities detailed in Section 1.6; and the organic layers provide intrinsic passivation of the inorganic slab surfaces, reducing trap-state densities at the heterojunction interfaces . The price paid is a modest reduction in charge-carrier mobility relative to three-dimensional analogs, since carriers must traverse the organic-inorganic boundaries. Chapter [ch:perovskite_detectors] investigates whether surface-passivation strategies can recover sufficient transport quality to enable practical detector operation while retaining the stability advantages of the 2D architecture.

### Methylhydrazinium Lead Chloride (MHyPbCl​3)

Methylhydrazinium lead chloride, MHyPbCl​3 (MHy​+ = CH​3NH​2NH​2+), is a relatively recently reported member of the halide perovskite family in which the conventional monovalent cation is replaced by the methylhydrazinium ion . This composition is of particular interest for fast-neutron detection because of its exceptionally high hydrogen content: the CH​3NH​2NH​2+ cation carries five hydrogen atoms, and the resulting crystallographic hydrogen density is approximately 3.79×1022 H cm​−3 . This exceeds the hydrogen density of many purpose-built neutron moderator and detector materials. Fast neutrons (energies above ∼1 MeV) interact primarily with hydrogen nuclei via elastic scattering, transferring up to 100% of their kinetic energy to the recoil proton in a head-on collision; those recoil protons then ionize the detector medium in the same manner as a directly ionizing particle. The combination of high hydrogen density (for neutron moderation and proton production), moderate bandgap (∼3.0 eV, appropriate for room-temperature operation), and the semiconducting perovskite framework (for direct electronic readout) makes MHyPbCl​3 a compelling candidate for a compact direct-conversion fast-neutron detector. Chapter [ch:perovskite_detectors] presents the synthesis, characterization, and fast-neutron response measurements for this material.

## Radiation Detection Fundamentals

### Mechanisms of Ionizing Radiation Detection

A radiation detector converts the energy deposited by an ionizing particle or photon into a measurable quantity, in semiconductor detectors, this quantity is an electrical charge pulse whose amplitude is proportional to the deposited energy. The process proceeds in three stages: (1) the primary ionizing event, in which the incident radiation transfers energy to the detector medium, producing a spatial distribution of electron-hole pairs along the particle track or at the absorption site; (2) charge transport, in which the liberated carriers drift under the applied bias field toward the collection electrodes; and (3) signal induction and readout, in which the moving charges induce a current pulse on the electrodes that is amplified and digitized .

The mean energy required to create one electron-hole pair in a semiconductor is given by Klein’s empirical rule,

$$\begin{equation}
      W \approx 2.67\,E_{\rm g} + 0.87~\text{eV},
      \label{eq:klein}
    \end{equation}$$

where $E_{\rm g}$ is the bandgap energy . For MAPbI​3 ($E_{\rm g} \approx 1.55$ eV), this gives W≈5.0 eV per pair; for CsPbBr​3 ($E_{\rm g} \approx 2.3$ eV), W≈7.0 eV per pair. These values compare favorably with conventional semiconductor detectors: silicon (W=3.6 eV) and germanium (W=2.9 eV) produce more pairs per unit energy, but those materials require cryogenic cooling or high-purity growth technologies incompatible with cost-effective deployment. The higher W of perovskites is partially offset by their far greater stopping power per unit thickness (Section 1.4), so the total charge produced by a given photon energy can be comparable to or exceed that in a thinner silicon detector despite the higher pair creation energy.

### Energy Resolution and Pulse Height Analysis

The ability to resolve closely spaced photon energies, and thereby identify specific radionuclides, is quantified by the energy resolution R, conventionally expressed as the fractional full-width at half-maximum (FWHM) of a spectral peak:

$$\begin{equation}
      R = \frac{\Delta E_{\rm FWHM}}{E_0},
      \label{eq:resolution}
    \end{equation}$$

where E0 is the incident photon energy. In an ideal semiconductor detector in which Poisson statistics govern pair production, the minimum achievable resolution is set by the Fano limit:

$$\begin{equation}
      \Delta E_{\rm FWHM}^{\rm Fano} = 2.35\,\sqrt{F \cdot W \cdot E_0},
      \label{eq:fano}
    \end{equation}$$

where F is the Fano factor (F≈0.1–0.2 for most semiconductors) . In practice, the measured resolution is degraded by incomplete charge collection due to carrier trapping, electronic noise from the amplifier chain, and dielectric polarization from ion migration (the last factor being specific to halide perovskites and discussed in Section 1.6). The benchmark figure commonly cited in the perovskite detector literature is the 1.4% resolution at 662 keV (​137Cs) achieved by He et al. for a CsPbBr​3 single crystal coupled to a custom application-specific integrated circuit (ASIC) , which at the time of publication was the best room-temperature resolution demonstrated by any non-CZT semiconductor detector.

Energy-resolved radiation measurements are performed by connecting the detector preamplifier output to a pulse-height analyzer (PHA), which bins each charge pulse by its amplitude and accumulates a histogram, the pulse-height spectrum, whose peak positions encode incident photon energies and whose areas are proportional to the detected activity. The shaping time of the amplifier is a critical parameter: it must be long enough to integrate the slow hole component of the charge pulse (hole mobilities in halide perovskites are typically 5–10× lower than electron mobilities) but short enough to avoid excessive pileup at practical count rates.

### X-Ray Detector Sensitivity

For applications in medical and industrial X-ray imaging, the relevant figure of merit is not energy resolution but sensitivity S, defined as the charge collected per unit area per unit X-ray exposure:

S=ΔQA⋅ΔX μC Gy−1 cm−2,

where ΔX is the absorbed dose rate. Sensitivity is controlled by the X-ray absorption efficiency (determined by the stopping power and detector thickness), the charge collection efficiency (determined by μτ products and applied field), and the dark current level (which sets the minimum detectable signal). Perovskite thick-film detectors fabricated from polycrystalline MAPbI​3 or MAPbBr​3 have demonstrated sensitivities exceeding 4,500 μC Gy​−1 cm​−2 under 8 keV X-rays, more than 104 times higher than conventional amorphous selenium panels . The high atomic number of the Pb sublattice is the primary driver of this extraordinary sensitivity at soft X-ray energies, where the photoelectric cross-section scales roughly as Z4.5.

### Neutron Detection and Discrimination

Neutron detection in semiconductor materials is indirect: neutrons carry no charge and interact negligibly with electrons, so they must first undergo a nuclear reaction or elastic scattering event that produces a charged secondary particle capable of ionizing the detector. Thermal neutrons (energies below ∼0.5 eV) are most efficiently captured via exothermic reactions such as ​10B(n,α)​7Li and ​6Li(n,α)​3H. Fast neutrons above ∼1 MeV interact principally through elastic scattering from hydrogen nuclei, producing recoil protons with a continuous energy spectrum up to the full neutron energy. The detection efficiency for fast neutrons is proportional to the hydrogen areal density in the active medium, making hydrogen-rich materials intrinsically advantageous. The measured ​1H density in MHyPbCl​3 of 3.79×1022 cm​−3 exceeds that of common polymer moderator materials and places this perovskite in a unique position as a combined moderating and detecting medium for fast neutrons .

Discrimination between neutron and gamma signals is accomplished by exploiting differences in the ionization density (linear energy transfer, LET) of the respective secondary particles. Recoil protons from fast-neutron elastic scattering and alpha particles from thermal capture reactions deposit energy far more densely than the Compton electrons produced by gamma photons of similar incident energy. In systems with sufficient time resolution, pulse-shape discrimination (PSD) can separate the fast and slow scintillation components that arise from these different ionization densities; in solid-state detectors, differences in carrier extraction dynamics under the high local ionization density of heavy charged particles can be exploited in a similar manner .

## Wide Bandgap Semiconductors for Room-Temperature Detection

### The Room-Temperature Constraint

The operating requirement most often overlooked in academic detector comparisons, yet most consequential for deployment in nuclear plants, field instruments, and space systems, is that the detector must function reliably at room temperature without active cooling. This single constraint eliminates two of the highest-performing semiconductor detector technologies: germanium (HPGe) must be operated below 120 K to suppress thermally generated leakage current, requiring liquid-nitrogen dewars or mechanical cryocoolers that add cost, mass, and failure modes incompatible with unattended monitoring . Silicon drift detectors, while operable at modest Peltier cooling (−20 to −40 ∘C), still suffer from displacement damage under high neutron fluences that degrade their spectroscopic performance irreversibly.

The root cause of the temperature sensitivity in narrow-gap semiconductors is the intrinsic carrier concentration ni, which increases exponentially with temperature as:

$$\begin{equation}
      n_i = \sqrt{N_c N_v}\,\exp\!\left(-\frac{E_{\rm g}}{2kT}\right),
      \label{eq:ni}
    \end{equation}$$

where Nc and Nv are the effective density of states in the conduction and valence bands, respectively, and k is Boltzmann’s constant . At room temperature (T=300 K), germanium ($E_{\rm g} = 0.67$ eV) has ni≈2.4×1013 cm​−3, producing a leakage current density many orders of magnitude larger than the signal currents from typical radiation fields. Silicon ($E_{\rm g} = 1.12$ eV) fares considerably better with ni≈1.5×1010 cm​−3, but displacement damage from neutron irradiation introduces compensating defects that effectively raise the intrinsic carrier density and degrade the depletion voltage over time.

For a semiconductor to operate as a room-temperature detector without active cooling or impractically high reverse bias, ni must be sufficiently low that the thermal generation current is smaller than the smallest radiation-induced signal of interest. A widely cited rule of thumb requires ni≲107 cm​−3, which for silicon-like band structure translates to a minimum bandgap of approximately 1.5 eV . This threshold defines the wide bandgap semiconductor regime relevant to room-temperature radiation detection.

### Figures of Merit for Wide Bandgap Detector Materials

The suitability of a wide bandgap semiconductor for radiation detection is characterized by several interrelated figures of merit beyond the bandgap itself:

Resistivity (ρ, Ω cm). High bulk resistivity minimizes the dark current $I_{\rm dark} = V/R = VA/(L\rho)$ that flows under the applied bias field and sets the noise floor. For spectroscopic applications, resistivities above 109 Ω cm are typically required; for imaging applications where high flux dominates shot noise, values above 107 Ω cm may be acceptable. Wide bandgap materials achieve high resistivity by a combination of large $E_{\rm g}$ (reducing ni) and the absence of shallow donor or acceptor impurities in the bandgap. CsPbBr​3 single crystals have been measured at ρ>1010 Ω cm at room temperature , exceeding the resistivity of commercial CdZnTe by approximately one order of magnitude.

Mobility-lifetime product (μτ, cm​2 V​−1). As derived in Section 1.4.2, μτ directly governs the mean free path of carriers between generation and trapping events. Wide bandgap semiconductors generally have lower carrier mobilities than narrow-gap materials (because heavier effective masses accompany larger bandgaps in many crystal systems), but the lifetime can be extraordinarily long in materials with low defect densities, partially compensating. The target for spectroscopic detectors is μeτe≳10−3 cm​2 V​−1; for hole collection, the equivalent target is often relaxed to 10−4 cm​2 V​−1 when single-polarity collection schemes are employed .

Effective atomic number ($Z_{\rm eff}$). For gamma and X-ray detection, $Z_{\rm eff}$ determines the photoelectric stopping power, which scales as Z4.5. Wide bandgap semiconductors based on heavy elements (Pb, Bi, Hg, Cd, Te) combine the thermal benefits of a large bandgap with high stopping power in a way that narrow-gap elemental semiconductors cannot achieve. Silicon (Z=14) requires centimeters of active thickness to stop 662 keV photons, while a few millimeters of CsPbBr​3 ($Z_{\rm eff} = 65.9$) or CdZnTe ($Z_{\rm eff} = 49.1$) provide equivalent absorption .

Pair creation energy (W, eV). As noted in Eq. [eq:klein], W is approximately proportional to $E_{\rm g}$. Wide bandgap materials therefore produce fewer electron-hole pairs per unit of deposited energy than narrow-gap ones, increasing the statistical (Fano) contribution to the energy resolution. This is the principal penalty paid for room-temperature operability: it must be offset by large μτ products that ensure complete charge collection, since any additional variance from trapping further degrades the resolution beyond the Fano limit.

### The Wide Bandgap Material Landscape

Table 1.1 contextualizes the halide perovskites investigated in this dissertation within the wider landscape of wide bandgap semiconductor detector materials.

Selected properties of wide bandgap semiconductor detector materials at 300 K. CZT = cadmium zinc telluride Cd​0.9Zn​0.1Te. Data compiled from .

| Material | $E_{\rm g}$ (eV) | $Z_{\rm eff}$ | ρ (Ω cm) | μeτe (cm​2 V​−1) | W (eV) | Best R662 |
| --- | --- | --- | --- | --- | --- | --- |
| Si | 1.12 | 14 | >104 | >1 | 3.6 | <0.1% (cryo) |
| CdTe | 1.50 | 49.5 | 109 | 3×10−3 | 4.4 | 1.7% |
| CZT | 1.57 | 49.1 | 1010 | 10−2 | 4.6 | 0.5% |
| GaAs | 1.42 | 31.6 | 107 | 10−5 | 4.2 | ∼2% |
| 4H-SiC | 3.26 | 14 | >1012 | 10−6 | 8.0 | ∼1%* |
| HgI​2 | 2.13 | 62.2 | 1013 | 10−4 | 4.2 | 0.5% |
| CsPbBr​3 | 2.30 | 65.9 | >1010 | 1.3×10−2 | 7.0 | 1.4% |
| MAPbI​3 | 1.55 | 51.4 | 108 | 8×10−3 | 5.0 | ∼6% |
| For alpha particles; gamma spectroscopy performance is limited by the low $Z_{\rm eff}$. |  |  |  |  |  |  |

Several observations emerge from this comparison. CdZnTe has long occupied the upper tier of room-temperature gamma spectrometers, combining a near-ideal bandgap for thermal leakage suppression, high $Z_{\rm eff}$, and a μeτe product sufficient for millimeter-to-centimeter-scale crystals, but its dominance rests entirely on the extraordinary effort invested in Bridgman crystal growth and post-growth processing that has accumulated over three decades. HgI​2 offers the highest $Z_{\rm eff}$ and resistivity of the conventional materials but suffers from mechanical fragility and a phase transition at 127 ​∘C that has limited commercial uptake. Silicon carbide (4H-SiC) is exceptional in its radiation hardness and thermal tolerance but its low $Z_{\rm eff}$ confines it to charged-particle and neutron applications where stopping power from the heavy-element sublattice is not required .

CsPbBr​3 occupies a remarkably favorable position in this landscape. Its $Z_{\rm eff}$ of 65.9 is the highest of any material in common laboratory study, its μeτe is competitive with CdZnTe despite far simpler solution-based crystal growth, and its resistivity exceeds that of CdZnTe by an order of magnitude. The 1.4% energy resolution at 662 keV achieved by He et al. is already within a factor of three of the best CdZnTe single-element detectors, and it was achieved after only a few years of focused development . The remaining gap is attributable primarily to the ion-migration polarization effect (Section 1.6), which introduces a time-dependent component to charge collection efficiency not present in purely electronic semiconductors.

### Why Bandgap Engineering Matters: The Perovskite Advantage

The halide perovskite family is unique among wide bandgap detector candidates in that the bandgap is continuously tunable over the range 1.2–3.5 eV by compositional substitution at all three crystallographic sites, without changing the crystal structure or growth method. Replacing iodide with bromide shifts the bandgap from 1.55 eV (MAPbI​3) to 2.3 eV (MAPbBr​3); substituting Pb​2+ with Sn​2+ narrows the gap to ∼1.2 eV; replacing MA​+ with the larger FA​+ cation narrows the gap marginally to ∼1.48 eV . This tunability enables the optimization of three competing requirements simultaneously: (1) $E_{\rm g}$ large enough to suppress thermal leakage at the maximum operating temperature; (2) $E_{\rm g}$ small enough to keep W, and therefore the Fano noise, acceptably low; and (3) $Z_{\rm eff}$ high enough for efficient photon stopping in the energy range of interest. No other material family offers all three degrees of freedom within a single, solution-processable crystal system, which is the central motivation for investigating multiple perovskite compositions across the chapters that follow.

## Radiation Interaction with High-Z Semiconductors

### Photon Interactions

Three mechanisms govern the interaction of gamma and X-ray photons with matter: the photoelectric effect, Compton scattering, and pair production. Each dominates over a different energy range and scales differently with the atomic number of the absorber, making the choice of detector material central to the detection efficiency for a given source energy.

The photoelectric effect is dominant below approximately 100 keV in high-Z materials. An incident photon is completely absorbed by an inner-shell electron, which is ejected with kinetic energy Ee=hν−Eb, where Eb is the binding energy of that shell. The photoelectric cross-section scales strongly with atomic number and inversely with photon energy as $\sigma_{\rm pe} \propto Z^{4.5}/E^{3.5}$, so high-Z semiconductors provide orders-of-magnitude higher photoelectric absorption than silicon or germanium for the same detector volume. The complete energy deposition of the photoelectric process produces the full-energy peak in the pulse-height spectrum, making it the principal mechanism for photon spectroscopy.

Compton scattering dominates for photon energies between approximately 100 keV and several MeV in heavy materials. An incident photon transfers a fraction of its energy to a loosely bound or free electron, with the scattered photon carrying the remainder. Because only partial energy is deposited, Compton events populate a continuum below the full-energy peak rather than contributing to it. The Compton cross-section is proportional to Z, so high-Z absorbers still offer a substantial geometric advantage, but the spectroscopic information is contained only in the photopeak fraction.

Pair production becomes significant above the threshold energy of 1.022 MeV and dominates at multi-MeV photon energies. The photon is converted into an electron-positron pair in the Coulomb field of the nucleus; the 511-keV annihilation photons from the subsequent positron annihilation appear as characteristic escape peaks in the spectrum. The pair-production cross-section scales as Z2.

The combined effect of these mechanisms is captured by the mass attenuation coefficient μ/ρ, tabulated as a function of energy for all elements by the National Institute of Standards and Technology (NIST XCOM database). For a compound material, the effective atomic number is calculated as:

$$\begin{equation}
      Z_{\rm eff} = \left(\sum_i w_i Z_i^n\right)^{1/n},
      \label{eq:Zeff}
    \end{equation}$$

where wi is the weight fraction of element i and the exponent n≈3.5 is chosen to match the photoelectric cross-section scaling . Applying this formula to CsPbBr​3 (Cs: Z=55, Pb: Z=82, Br: Z=35; stoichiometric weight fractions of 0.229, 0.449, and 0.322, respectively) yields $Z_{\rm eff} \approx 65.9$, substantially higher than silicon ($Z_{\rm eff} = 14$), germanium (32), or even CdZnTe ($Z_{\rm eff} \approx 49.1$) .

### Charge Transport and the Hecht Equation

Even if radiation deposits charge in the bulk of a detector, that charge must be transported to the collection electrodes without recombination or trapping if a proportional signal is to be measured. The quality of charge transport is characterized by the mobility-lifetime product μτ for electrons and holes separately. Carrier mobility μ (cm​2 V​−1 s​−1) quantifies the drift velocity per unit electric field; carrier lifetime τ (s) is the mean time before a carrier is irreversibly trapped at a deep defect and removed from the circuit. The product μτ has units of cm​2 V​−1 and represents the mean distance a carrier drifts per unit of applied field before being trapped; a large μτ indicates that carriers can traverse a thick crystal without significant charge loss.

The fractional charge collection for a detector of thickness L under applied field E can be derived rigorously for a planar single-carrier case. For a general double-carrier detector with the interaction site at depth x from the cathode, the Hecht equation gives:

Q(x)=Q0μeτeEL1−e−(L−x)/μeτeE+μhτhEL1−e−x/μhτhE,

where Q0=eN0 is the charge generated by the initial ionizing event . For uniform irradiation, averaging Eq. [eq:hecht] over x from 0 to L gives the mean charge collection efficiency (CCE), which approaches unity only when both μeτeE/L≫1 and μhτhE/L≫1. In practice this requires either very high applied fields, very thin detectors, or very large μτ products.

Halide perovskites have demonstrated μτ products competitive with those of mature compound semiconductors. Single-crystal MAPbI​3 exhibits μeτe≈8×10−3 cm​2 V​−1 and μhτh≈3×10−3 cm​2 V​−1 , values that in a 1-mm-thick crystal at a modest field of 100 V cm​−1 yield a mean electron drift length of ∼8 mm, far exceeding the crystal thickness. CsPbBr​3 single crystals have achieved μeτe up to 1.34×10−2 cm​2 V​−1, supporting the 1.4% energy resolution reported by He et al. . These values are within a factor of two to three of CdZnTe (μeτe∼10−2 cm​2 V​−1), a material that has required decades of crystal growth refinement to achieve its current performance levels.

The hole transport is typically the limiting factor in halide perovskites, as in most compound semiconductors. The hole μτ in both MAPbI​3 and CsPbBr​3 is typically 5–10× lower than the electron value, leading to a characteristic single-polarity collection signature in which events occurring near the cathode (from which electrons must traverse the full crystal thickness) are preferentially detected. Electronic techniques such as single-carrier collection (using a Frisch collar or virtual Frisch ring) and waveform analysis can mitigate poor hole collection , and perovskite detectors are amenable to these approaches.

## Schottky Diode Contacts in Semiconductor Detectors

### Metal-Semiconductor Junction Physics

When a metal is brought into contact with a semiconductor, charge redistributes at the interface until the Fermi levels align, creating a built-in potential difference and a depletion region in the semiconductor. For a metal in contact with an n-type semiconductor, the Schottky barrier height is:

$$\begin{equation}
      \phi_{\rm B} = \phi_m - \chi_s,
      \label{eq:schottky_barrier}
    \end{equation}$$

where ϕm is the metal work function and χs is the electron affinity of the semiconductor . The depletion region extends a distance W into the semiconductor:

$$\begin{equation}
      W = \sqrt{\frac{2\varepsilon\varepsilon_0 (V_{\rm bi} - V)}{e N_D}},
      \label{eq:depletion_width}
    \end{equation}$$

where ε is the static dielectric constant, $V_{\rm bi}$ is the built-in voltage, V is the applied reverse bias, and ND is the donor concentration. The rectifying current-voltage relationship of the Schottky diode follows the thermionic emission model:

$$\begin{equation}
      J = J_0\left(e^{qV/nkT} - 1\right), \quad
      J_0 = A^{**}T^2\,e^{-q\phi_{\rm B}/kT},
      \label{eq:IV_schottky}
    \end{equation}$$

where A** is the effective Richardson constant and n is the ideality factor .

In contrast, an ohmic contact is formed when the metal work function is matched to the Fermi level of the semiconductor such that no barrier to majority-carrier flow exists. Ohmic contacts allow free exchange of majority carriers with the external circuit and are necessary on the collection side of the detector to avoid field distortion near the electrode.

### Application to Halide Perovskite Detectors

The asymmetric contact architecture, one ohmic and one Schottky electrode, has become the standard configuration for halide perovskite radiation detectors because it simultaneously achieves low dark current and efficient charge collection . Under reverse bias, the Schottky junction is depleted, suppressing majority-carrier injection from the blocking contact; minority carriers generated by ionizing radiation within the depletion region are swept by the electric field toward the appropriate electrode. Because the dark current is thermally limited by the Schottky barrier rather than set by the bulk resistivity, even moderate barrier heights of 0.5–0.8 eV can reduce the dark current density by several orders of magnitude relative to the ohmic-contact geometry.

For MAPbI​3-based detectors, gold (Au, ϕm=5.1 eV) forms a near-ohmic contact on the p-type surface, while chromium (Cr, ϕm=4.5 eV), gallium, or indium contacts on the opposite face exhibit Schottky character . For CsPbBr​3, the typical asymmetric pair is a carbon paste or Au ohmic contact on one face and a Ga or indium-gallium eutectic Schottky contact on the other. The net result is a device structure functionally analogous to a p-i-n junction in which the intrinsic region (the semi-insulating bulk crystal) contains the active detector volume, and the contact asymmetry enforces unipolar drift under bias .

For the 2D perovskite devices studied in Chapter [ch:perovskite_detectors], the layered crystal architecture introduces an additional consideration: charge transport perpendicular to the organic spacer layers (the out-of-plane direction, which is the relevant direction for planar detector geometry) is more resistive than in-plane transport, and the contact interface with the topmost organic spacer layer must be carefully engineered to avoid a secondary barrier that would impede collection. Surface passivation using Lewis-base molecules that coordinate to surface Pb​2+ sites can simultaneously reduce trap-state density and tune the contact work function alignment.

## Ion Migration in Halide Perovskites

### Origins and Mechanisms

The same structural softness that enables solution-processable crystal growth from precursor salts also makes halide perovskites susceptible to ionic transport under applied fields, a property that distinguishes them fundamentally from conventional covalent or ionic semiconductors such as silicon or CdZnTe. Density functional theory calculations and activation energy measurements converge on halide vacancy migration as the dominant ionic conduction mechanism, with activation energies of approximately 0.1–0.6 eV depending on the halide and A-site cation . For comparison, the thermal energy at room temperature (kT≈26 meV) is sufficient to drive significant vacancy hopping across these barriers on detector-relevant timescales, particularly under the electric fields of 10–1,000 V cm​−1 routinely applied to semiconductor detectors.

The migration pathway for iodide vacancies in MAPbI​3 proceeds via nearest-neighbor hopping through the faces of the PbI​6 octahedra, with a computed activation barrier of approximately 0.58 eV . Bromide vacancies in CsPbBr​3 have a somewhat higher barrier of ∼0.74 eV, consistent with the greater thermal stability of that compound. Chloride vacancies, which are the operative mobile species in MHyPbCl​3, have not been as extensively studied computationally, but experimental activation energies inferred from temperature-dependent dark current measurements suggest similar or slightly higher barriers than for iodide.

### Consequences for Detector Performance

Ion migration manifests in detector operation through three interrelated phenomena. First, under sustained bias, mobile ions drift to the electrodes and accumulate, establishing an internal dipole that screens the applied field and reduces the effective field within the crystal bulk. This polarization effect depresses charge collection efficiency over time and produces the characteristic dark current spike followed by slow decay observed in the current transient of a freshly biased perovskite crystal . Second, the accumulation of ions at the electrode interfaces modifies the contact barrier height, causing the rectification ratio and dark current to evolve continuously during operation, a direct threat to the baseline stability required in nuclear instrumentation. Third, if the bias polarity is reversed (as during AC-coupled readout or impedance spectroscopy measurements), the accumulated ion profiles transiently drive the internal field in the opposite direction to the intended collection field, producing severe measurement artifacts.

These effects are not merely theoretical concerns: in a systematic study of CsPbBr​3 single-crystal detectors, Pan et al. demonstrated that the charge collection efficiency under a fixed field of 200 V cm​−1 dropped by approximately 30% over the first 100 seconds of bias application before reaching a new quasi-equilibrium dominated by ionic rather than electronic currents . The voltage-induced degradation was partially reversible upon removal of bias, with recovery occurring on timescales of minutes to hours, consistent with thermal relaxation of the accumulated ion profiles .

### Mitigation Strategies

Several strategies have been demonstrated to suppress or circumvent ion-migration instability in perovskite detectors. 2D spacer layers (the Ruddlesden-Popper architecture) interpose wide-gap organic bilayers at regular intervals through the crystal thickness, acting as electrostatic barriers to halide vacancy drift while preserving charge transport via tunneling or thermally activated hopping . Surface passivation with Lewis-base ligands such as phenethylammonium iodide (PEAI), methylammonium chloride, or thiophene-2-carboxylic acid coordinates unsaturated surface Pb​2+ sites that would otherwise serve as ion-migration nucleation points and electronic trap states . All-inorganic compositions such as CsPbBr​3 exhibit significantly slower ion drift than their hybrid organic-inorganic analogs because the rigid Cs​+ sublattice provides fewer low-energy migration pathways. Finally, low-temperature operation reduces the ionic conductivity exponentially (Arrhenius behavior) and has been used to virtually eliminate polarization artifacts in experimental detector characterizations, though at the cost of the room-temperature operability that is one of perovskite’s primary advantages . Chapter [ch:perovskite_detectors] investigates the combination of 2D architecture with chemical surface passivation as a room-temperature solution to the voltage-induced instability problem.

## Prior Art in Perovskite Radiation Detectors

### Early Single-Crystal Gamma Detectors

The first demonstration of halide perovskite single crystals as room-temperature radiation detectors appeared in a pair of landmark papers in 2016. Wei et al. grew large MAPbI​3 single crystals by inverse temperature crystallization and contacted them in an asymmetric Au/perovskite/Cr geometry; at 662 keV they observed a resolved ​137Cs photopeak with an energy resolution of approximately 6.8% . While this was inferior to the best CdZnTe devices, the demonstration that a solution-processed hybrid perovskite could rival polycrystalline CdZnTe, at a fraction of the material cost and with far simpler growth conditions, generated immediate and sustained interest. Concurrently, Yakunin et al. reported sensitivity values exceeding 103 μC Gy​−1 cm​−2 for MAPbI​3 thick-film X-ray detectors, establishing the perovskite platform for medical and industrial X-ray imaging .

### CsPbBr​3 and the Resolution Record

The shift from hybrid to all-inorganic CsPbBr​3 was motivated by the thermal and photo-instability of MAPbI​3, which loses iodide at temperatures above ∼85 ​∘C and degrades rapidly in ambient humidity. Pan et al. demonstrated in 2019 that centimeter-scale CsPbBr​3 single crystals grown by the Bridgman method exhibit a resistivity exceeding 109 Ω cm, μeτe products above 10−2 cm​2 V​−1, and a 662 keV energy resolution of approximately 3.9% . The subsequent integration of CsPbBr​3 detectors with custom-designed ASICs, rather than laboratory charge-sensitive amplifiers, addressed the electronic noise limitation and enabled the record 1.4% resolution at 662 keV reported by He et al. in 2021 , subsequently approached and extended by other groups employing refined crystal growth and improved contact engineering .

### X-Ray Detection and Imaging

Polycrystalline thick films of MAPbI​3, MAPbBr​3, and CsPbI​2Br have been investigated extensively as direct-conversion X-ray detector arrays for applications in digital radiography and computed tomography. The high atomic number of the Pb sublattice confers exceptional sensitivity at soft X-ray energies (below ∼30 keV), where the photoelectric cross-section makes lead-bearing compounds intrinsically more absorbing than the amorphous selenium currently deployed in flat-panel detectors. Wei et al. reported a sensitivity of 4,500 μC Gy​−1 cm​−2 for a 2-mm-thick solution-processed MAPbI​3 film under an 8 keV X-ray beam , and subsequent optimization of film deposition and contact passivation has pushed sensitivities above 10​4 μC Gy​−1 cm​−2 in several laboratories. The principal challenges remaining for commercial deployment are long-term operational stability (particularly under the high photon fluences of medical imaging), the toxicity of lead-bearing materials in a clinical environment, and the uniformity of thick-film deposition over large detector areas.

### Neutron Detection

Neutron detection by perovskite materials has been demonstrated via two complementary approaches: neutron-capture via the incorporation of ​10B or ​6LiI into the perovskite matrix, and direct fast-neutron detection via hydrogen-recoil in hydrogen-rich perovskites. The composite approach was demonstrated in this group’s own prior work: MAPbI​3 crystals incorporating hexagonal boron nitride (hBN) nanoflakes were shown to exhibit a measurable response to thermal neutrons, with the neutron signal distinguished from the ambient gamma background by pulse-shape analysis . The MHyPbCl​3 results reported in Chapter [ch:perovskite_detectors] represent the first systematic investigation of a perovskite designed from the outset for high hydrogen content, aiming to maximize the fast-neutron elastic-scatter cross-section in a single-phase semiconducting medium. The availability of a structurally well-characterized perovskite with both high H density and a bandgap suitable for room-temperature electronic detection opens a path toward compact direct-conversion fast-neutron detectors that do not require external moderators or ​3He-filled proportional tubes.

### Mixed-Cation and 2D Detector Architectures

The instability of single-phase 3D perovskites under sustained bias has driven interest in compositionally engineered architectures designed to suppress ion migration while retaining the favorable electronic properties of the perovskite host. Two-dimensional Ruddlesden-Popper compounds were first applied to radiation detection by Xu et al., who demonstrated that PEA​2MA​3Pb​4I​13 (n=4) single crystals exhibited suppressed polarization current compared to 3D MAPbI​3 under identical bias conditions, attributed to the PEA​+ barriers impeding halide vacancy drift . The compositions studied in Chapter [ch:perovskite_detectors] extend this concept to the n=3 compound PEA​2MA​2Pb​3I​10, where the additional organic layer density provides even stronger suppression of ion migration, and investigates the interaction between the 2D architecture and chemical surface passivation as a dual strategy for achieving stable, low-dark-current detector operation.

## Summary

This chapter has established the conceptual framework necessary to interpret the experimental results reported in Chapters [ch:CsFAPbI] and [ch:perovskite_detectors]. The ABX​3 halide perovskite framework accommodates a diverse family of compositions spanning 3D, quasi-2D, and layered architectures, with A-site chemistry tunable from inorganic Cs​+ through hybrid organic-inorganic MA​+ and FA​+ to the hydrogen-rich methylhydrazinium cation of MHyPbCl​3. The physics of semiconductor radiation detectors connects material properties, bandgap, effective atomic number, μτ product, to measurable figures of merit such as energy resolution, sensitivity, and neutron detection efficiency via the Hecht equation and Klein’s pair-creation rule. The Schottky diode contact architecture suppresses dark current to levels compatible with radiation counting without sacrificing charge collection, provided that ion migration is controlled by compositional engineering or surface passivation. The problem of voltage-induced instability driven by halide vacancy migration is identified as the central unsolved challenge for room-temperature perovskite detector operation, motivating the 2D and passivation strategies pursued in the experimental chapters that follow. The experimental investigation begins in Chapter [ch:CsFAPbI] with photovoltaic-architecture perovskite solar cells operating as current-mode monitors at zero bias, establishing the radiation-response baseline before Chapter [ch:perovskite_detectors] introduces the applied-bias, direct-conversion detector geometries that enable pulse-by-pulse energy spectroscopy.